ARDEX GUIDE SPECIFICATION

ARDEX ProDrain® Drainage System

Exterior, On Open Grade Base to Receive a Drainage System for the

Installation of Tile and Stone Pavers

SECTION 320000

ARDEX TILE & STONE INSTALLATION EXTERIOR DRAINAGE MATERIALS AND

SYSTEMS

PART 1 - GENERAL

1.1	RELATED DOCUMENTS

A.	Drawings, general provisions of the Contract, and other related construction documents such as Division 01 specifications apply to this Section

1.2	SUMMARY

A.	This Section includes the installation of ARDEX ProDrain® Drainage Mortar System over an exterior, open grade base  prior to installing tile and stone pavers with a mortar

- ARDEX UE 195-10 ProDrain® Drainage Mat

- ARDEX UD 158 ProDrain® Reinforcement Tape

- ARDEX ProFin Series Edge Strip

- ARDEX US 422 ProDrain AB-V Tape

- ARDEX A 14TM Drainage Mortar / ARDEX A 11™ Drainage Mortar

- ARDEX X 90 OUTDOOR™ MicroteC3 Rapid-Set, Flexible Tile and Stone Mortar

- ARDEX FL™ Rapid Set, Flexible, Sanded Grout

- ARDEX FH™Sanded Grout

9.	ARDEX SX™ 100% Silicone Sealant for Tile and Stone Applications

B.	Complete ARDEX product and system installation details are provided in their corresponding Technical Data Sheet available at www.ardexamericas.com.

C.	Related Sections include the following:

- Division 09 Tile & Stone Sections

- Division 32 Exterior Improvements

1.3	REFERENCES

A.	AMERICAN NATIONAL STANDARDS INSTITUTE (A.N.S.I.)

- A-118.15 Improved Modified Dry-Set Cement Mortar

- A-118.6 Standard Cement Grout

- A-118.7 High Performance Cement Grouts for Tile Installation

- A-108.01 General Requirements for Subsurfaces and Preparations by Other Trades

- A-108.10 Installation of Grout in Tilework

D.	TILE COUNCIL OF NORTH AMERICA, INC.

1.	Handbook for Ceramic Tile Installation

E.	INTERNATIONAL STANDARDS ORGANISATION (ISO)

1.	ISO 13007 – Ceramic Tile-Grouts & Adhesives 
1.4 SUBMITTALS

- Product Data: Submit manufacturer's product data, a Revit file with applicable materials meeting the Revit Content Style Guide, and installation instructions for each material and product used. Include manufacturer’s Safety Data Sheets.

- Qualification Data: For Installer

1.5	QUALITY ASSURANCE

- Installation of the ARDEX ProDrain System must be completed by -trained installers per manufacturers instructions and completed check list

1.6	WARRANTY: When ARDEX UE 195-10 ProDrain® is used in conjunction with ARDEX A 14™/ ARDEX A 11™ Drainage Mortar, ARDEX X 90™, and ARDEX FH™/ ARDEX FL™ Grout , the drainage system will not break down or disbond due to manufacturing or formulation defect for 5 years from the date of installation. See the ARDEX Exterior Drainage Systems Warranty for full warranty details.

1.7	DELIVERY, STORAGE AND HANDLING

- Deliver products in original packaging, labeled with product identification, manufacturer, batch number and shelf life.

- Store products in a dry area with temperature maintained between 50° and 85°F (10° and 29°C) and protect from direct sunlight.

- Handle products in accordance with manufacturer's printed recommendations.

1.8	PROJECT CONDITIONS

- Do not install material below 50°F (10°C) surface and air temperatures. These temperatures must also be maintained during and for 48 hours after the installation of products included in this section. Install quickly if sub-base  is warm and follow warm weather instructions available from the ARDEX Technical Service Department.

- When ARDEX ProDrain® systems is to be installed over occupied spaces, an intact primary roofing membrane must be installed and in place prior to the installation of the ARDEX ProDrain® system (by others).

PART 2 – PRODUCTS

2.3	DRAINAGE MAT

A.	Acceptable Products:

1. ARDEX UE 195-10 ProDrain® Drainage Membrane; Manufactured by ARDEX AMERICAS , USA, (724) 203-5000, www.ardexamericas.com

2.4	SEAM REINFORCEMENT TAPE

A.	Acceptable Products:

1. ARDEX UD 158 ProDrain® Seam Reinforcement Tape; Manufactured by ARDEX AMERICAS , USA, (724) 203-5000, www.ardexamericas.com

2.5	PERIMETER STRIP

- ARDEX US 422 ProDrain AB-V Tape; Manufactured by ARDEX AMERICAS USA, (724)203-5000, www.ardexamericas.com

2.6	DRAINAGE MORTAR

A.	Acceptable Products:

- ARDEX A 14™; Manufactured by ARDEX AMERICAS USA, (724) 203-5000, www.ardexamericas.com

- ARDEX A 11™ Drainage Mortar; Manufactured by ARDEX AMERICAS USA, (724) 203-5000, www.ardexamericas.com

2.7	TILE or Stone Paver MORTAR

A.	Acceptable Products:

1.ARDEX X 90 ; Manufactured by ARDEX AMERICAS USA, (724) 203-

5000, www.ardexamericas.com

2.8	GROUT

A.	Acceptable Products:

1.ARDEX FL™ ; Manufactured by ARDEX AMERICAS USA, (724)

203-5000, www.ardexamericas.com

- ARDEX FH™; Manufactured by ARDEX AMERICAS USA, (724) 203-5000

2.9	Silicone Sealant

A. Acceptable Products:

1. ARDEX SX™; Manufactured by ARDEX AMERICAS USA, (724) 203-5000, www.ardexamericas.com

PART 3 – EXECUTION

3.1	PREPARATION

A.	Sub-base  : Prepare sub-base  in accordance with manufacturer’s instructions, industry standards

- ICPI (Interlocking Concrete Pavement Institute), CMHA or manufacturers design guides based on loading and soil conditions. Residential, pedestrian projects: patios, pool decks sidewalks and walkways. Not for commercial or vehicular applications. Sub-base  and ambient temperatures must be a minimum of 50°F (10°C). Sub-base soils to be permeable to prevent water from collecting and saturating the sub-base. Refer to ASTM D1557 general compaction compliant.

B.	Follow Manufacturer’s Technical Data sheets for installation of the ARDEX ProDrain® System, including sub-base  preparation, and installation of all components of the system.

3.2	CRACK AND JOINT PREPARATION

A.	All installations must include soft joints in accordance with  TCNA EJ 171.

3.3	MIXING SANDED MATERIALS

A.	When mixing sanded materials, ARDEX recommends using the ARDEX DUSTFREE™ or a standard “gutter hook” vacuum attachment in combination with a wet/dry (Shop-Vac® style) vacuum and HEPA dust extraction vacuum system. Additionally, each bag should be handled with care and emptied slowly to avoid creating a plume of dust.

3.4	SLOPING INSTALLATION (As needed)

3.5	VAPOR PROTECTION MEMBRANE INSTALLATION (Optional subject to project scope and

details. Contact ARDEX Technical for further details.)

- Install ARDEX TLT™ Waterproofing Membrane using ARDEX X 90  in accordance with the technical data sheet. Do not penetrate the membrane, including fixing any posts or railings once the draining system is installed.

- Comply with manufacturer's printed instructions for mixing of material, installation, and cure.

3.6	DRAINAGE MAT INSTALLATION

- Install ARDEX UE 195-10 ProDrain® Drainage Mat in accordance with the installation guide. in accordance with technical data sheet, including use of UD 158 ProDrain® Seam Reinforcement Tape, UD 146 Edge Insulation Strip  ARDEX US 422 ProDrain AB-V Tape

- Comply with manufacturer's printed instructions for mixing of material, installation, and cure.

3.7	APPLICATION OF DRAINAGE MORTAR WITH APPROVED REINFORCING MESH

(Approved reinforcing mesh is optional.)

- Install ARDEX A 14 / ARDEX A 11 in accordance with manufacturers printed instructions

- Comply with manufacturer's printed instructions for mixing of material, installation, and cure.

3.8	APPLICATION OF TILE or STONE PAVER

- Install Tile or Stone Paver with Mortar

1.	Install tile or stone pavers using ARDEX X 90  Comply with manufacturer’s printed instructions for mixing of materials, installation and cure. For questions contact the ARDEX Technical Services department (724)203-5000.

- Install Grout

- Install ARDEX FH or ARDEX FL in accordance with ANSI A108.10 . Grouting must not be applied around the perimeter edge.

- Comply with manufacturer's printed instructions for mixing of material, installation, and cure.

- Install Silicone Sealant

1.	Install ARDEX SX in accordance with manufacturers printed instructions. Comply with EJ171 movement joint guidelines.

3.9	FIELD QUALITY CONTROL

A.	If needed, contact manufacturer for field sampling methods and procedures. 
	3.10	PROTECTION & CLEANING

- Protect from abuse by other trades by the use of plywood, Masonite or other suitable protection course.

- Clean soiled surfaces using solution which will not harm tiles or pavers. Consult material supplier for recommendations. Use non-metallic tools for cleaning.

END OF SECTION