ARDEX GUIDE SPECIFICATION

ARDEX B 40™ Concrete Trench Repair Mortar

Fast-Setting Horizontal Concrete Repair Mortar

SECTION 03 92 50

REPAIR MORTARS

# PART 1 - GENERAL

## RELATED DOCUMENTS

## Drawings, general provisions of the Contract, and other related construction documents such as Division 01 specifications apply to this Section.

  - SUMMARY

- This Section includes Portland cement-based, polymer modified structural repair mortar with integral corrosion inhibitor.

  - ARDEX B 40™ Concrete Trench Repair Mortar

  - ARDEX EP 2000™ Substrate Preparation Primer

  - ARDEX BONDING & ANTI-CORROSION AGENT

- Related Sections include the following:

  - Section 03 30 00, Cast-In-Place Concrete

## REFERENCES

###### ASTM C 109, Compressive Strength of Hydraulic Cement Mortars

###### ASTM C 78, Flexural Strength of Concrete

###### ASTM C 4541, Direct Tensile Bond Strength

###### ASTM C 157, 28 days Length Change of Hardened Hydraulic-Cement Mortar and Concrete

          - ASTM C 882, Slant Shear Bond Strength

###### ICRI Technical Guideline No. 03732 Specifying Concrete Surface Preparation for Sealers, Coatings, and Polymer Overlays

###### ICRI Technical Guideline No. 03730 Guide for Surface Preparation for the Repair of Deteriorated Concrete Resulting from Reinforcing Steel Corrosion

## SUBMITTALS

## Product Data:  Submit manufacturer's product data and installation instructions for each material and product used.

## QUALITY ASSURANCE

## Manufacturer's Qualifications: The manufacturer shall be a company with at least five years experience and regularly engaged in the manufacture and marketing of products specified herein.

  - Installer should be experienced in performing specified work similar in design, products and scope of this project, with a documented track record of successful, in-service performance and with sufficient production capabilities, facilities and personnel to produce specified work.

## DELIVERY, STORAGE AND HANDLING

##### Deliver products in original packaging, labeled with product identification, manufacturer, batch number and shelf life.

##### Store products in a dry area with temperature maintained between 50° and 85° F (10° and 29° C) and Protect from direct sunlight.

##### Handle products in accordance with manufacturer's instructions.

## PROJECT CONDITIONS

          - Do not install material below 50° F (10° C) surface and air temperatures.  These temperatures must also be maintained during and for 48 hours after the installation of products included in this section.

# PART 2 - PRODUCTS

  - REPAIR MORTAR

##### Single-component, polymer-modified, Portland cement-based structural repair mortar, with integral corrosion inhibitors suitable for exterior and interior horizontal applications above, on or below grade.

###### Acceptable Products:

ARDEX B 40™; Manufactured by ARDEX Americas:  400 Ardex Park Drive, Aliquippa, Pa 15001 USA 724-203-5000

###### Performance and Physical Properties:  Meet or exceed the following values for material cured at 73° F (23° C) and 50 percent relative humidity:

### Application:  Trowel.

### Working Time:  25 – 45 minutes.

### Compressive Strength:  9300 psi (48.3MPa) at 7 days, 10,300 psi (56.58 MPa) at 28 days, ASTM C109.

### Flexural Strength: 1,200 psi (8.3 MPa) at 7 days, 1,250 psi (10.3 MPa) at 28 days, ASTM C293.

### Modulus of Elasticity:   3.43 x 106 psi at 28 days

### Color: Concrete gray.

# PART 3 – EXECUTION

##### PREPARATION

##### A. 	General: Prepare substrate in accordance with manufacturer’s instructions. Prior to proceeding with any repair, please refer to the International Concrete Repair Institute’s ICRI 03730 Guide for Surface Preparation for the Repair of Deteriorated Concrete Resulting from Reinforcing Steel Corrosion; ICRI 03732 Guideline for Selecting and Specifying Concrete Surface Preparation for Sealers, Coatings, and Polymer Overlays; and the American Concrete Institute’s ACI 546R-04 Concrete Repair Guide for general guidelines for concrete repair.

##### 1.	All concrete and masonry substrates must be sound, solid, dry, and completely free of all oil, grease, dirt, curing compounds and any substance that might act as a bond breaker.  Overwatered, frozen or otherwise weak concrete surfaces must also be cleaned down to sound, solid concrete by mechanical methods such as scarifying, scabbling or similar in accordance with ICRI 03732 before priming. Acid etching and the use of sweeping compounds and solvents are not acceptable.

###### 2. 	The repair area must be saw cut in a basic rectangular shape at least ¼” (6 mm) in depth.  The cuts should be made at 90° angle, and should be slightly keyed.  Chip out the concrete inside the cuts to a minimum depth of ¼” (6 mm) until the area is squared or box shape.

###### Mechanically prepare surface to obtain an exposed aggregate surface with a minimum surface profile of approximately 1/16” (1.5 mm).

###### For cases with exposed reinforcing steel, mechanically clean the steel to remove all rust and any other contaminants in accordance with ICRI 03730.  Prime the steel with ARDEX Bonding & Anti-Corrosion Agent™ prior to proceeding with repair.

B.	Joint Preparation

- Moving Joints and Cracks – honor all expansion and isolation joints up through the ARDEX B 40™.  A flexible sealing compound suitable for the application may be installed.  ARDEX ARDISEAL™ RAPID PLUS may be installed for interior applications only.

- Control Joints and dormant cracks greater than 1/16” – fill all non-moving joints and cracks with ARDEX ARDIFIX™ Joint Filler.

#### 3.2	APPLICATION OF ARDEX B 40™:

##### A.  	Examine substrates and conditions under which materials will be installed.  Do not proceed with installation until unsatisfactory conditions are corrected.

##### Coordinate installation with adjacent work to ensure proper sequence of construction.  Protect adjacent areas and landscaping from contact due to mixing and handling of materials.

        - Prepared concrete must be primed for bonded application of ARDEX B 24. For priming with ARDEX BACA or ARDEX EP 2000, follow the application instructions in the appropriate ARDEX technical data sheet. Please note that ARDEX BACA is suitable for a surface primer only. If ARDEX BACA is not used, use water to dampen the concrete until it is saturated thoroughly. When water is used, the goal is to saturate the pores of the concrete while leaving the surface free of liquid (SSD, Saturated Surface Dry). While the surface of the concrete must be dry and free of puddles, the pores of the concrete must be saturated with water. Installing the ARDEX B 24 over concrete that is dry can result in cracking and bond failure. Do not leave any bare spots. Brush or vacuum off puddles and excess liquid before installing.

##### Mixing:  Comply with manufacturer's printed instructions.

##### Application:  Comply with manufacturer's printed instructions.

###### Do not apply in freezing conditions or during precipitation.

###### Comply with manufacturer’s guides for hot and cold weather application.

###### Dampen substrate to fill concrete pores with water. Remove ponding, glistening, or surface water (saturated surface dry).

###### Apply scrub coat of repair mortar into substrate to ensure intimate contact and establish bond.

###### Apply ARDEX B 40™ while scrub coat is wet.  Consolidate and trowel to the desired finish.

###### ARDEX B 40™ can be installed to a minimum thickness of 1/2 inch up to 9” (12.7 mm to 22.86 cm) including full depth repairs up to 12” (30.48 cm), extend ARDEX B40™ by adding 25 pounds of clean, uniformly graded, ¼” to 3/8” pea gravel dampenend to an SSD condition.

##### Curing

###### Direct sunlight or wind may cause unwanted ARDEX B 24 surface drying. Avoid installation if rain or dew is expected within 6 - 8 hours. Keep the surface of the installation damp for 48 hours (light water fogging, curing blanket or curing compound). Do not allow water to puddle. Do not use solvent-borne curing compounds. Note: If the surface is to receive a topcoat or other type of finish, use moist curing methods only.

##### Cleaning:  Remove excess material before material cures.  If material has cured, remove using mechanical methods which will not damage substrate.

END OF SECTION